Мikulinska- Rudich Y. N., Mys V.O.

Experience of application of nanocomposite material in local enamel hypoplasia

Kharkov national medical university.

Department of pediatric dentistry, pediatric maxillofacial surgery and implantology.

Chief: M. D., professor Nazaryan R. S.

Topicality. Nanokomposite material Filtek Ultimate (3M ESPE), having excellent manipulative properties due to the unique patented technology nanofillers 3M ESPE. These technologies provide better light resistance material than microhybrid composite wear resistance higher than that of microhybrid material strength to withstand the stresses anterior and posterior teeth groups.

The purpose of our research is examine the effectiveness of the nanofilled composite material for the restoration of anterior teeth with carious lesions.

Materials and methods patient 17 years with complaints about a cosmetic defect of the front teeth and high aesthetic requirements for the future of the seal. An objective examination revealed loss of vestibular surface of the tooth 21 in the form of round-shaped patches of yellowish color. The boundaries of the spots clear, smooth surface. The thickness of the enamel in the spots is not changed. Probing painless. Spots dyes do not stain. The impact of temperature irritants does not cause pain. X-ray examination was conducted, as this form is not detected radiographically. On the basis of physical examination was diagnosed with a form of speckled enamel hypoplasia of moderate severity, limited turbidity.

We have proposed possible solutions to this problem:

1. Porcelain veneers - this method of recovery in this case is impossible, since the percentage of damaged hard tissues of the tooth is great

2. Dental crowns - a more reliable way to restore tooth structure, but talking about minimally invasive such designs are not quite appropriate.

3. Direct restoration composite. With the use of modern composite restoration can restore the anatomical shape of the teeth and achieve the desired aesthetics.

The advantage of direct composite restorations is a reasonable cost, speed of manufacture and minimally invasive compared with all-ceramic crowns.

In the course of planning the restoration we have identified mesiodistal tooth size for biomimetic method SV Radlinsky and color of the tooth- A2 in accordance with the scale VITA®.

Under the applicative (Benzocaine 20%) and infiltration anesthesia Sol. Ubistesini 4% -1,0 ml held grinding of the affected enamel. Cofferdam fixed using clamp for front teeth. Etching the cavity 15 seconds dentin, enamel for 30 seconds. Washing time 30 sec. Applying adhesive Adper Single Bond 2 (3M ESPE) for 15 seconds, drying air stream reapplication adhesive massaging for 30 seconds, polymerization for 10 seconds. Sealing using adhesive technique by light-curing restoration layered nanocomposite Filtek Ultimate: Filtek Ultimate Flowable A3, the main filling - Filtek Ultimate A2. To simulate light optical effects that are part of the natural tooth used flowable Filtek® Ultimate Flowable shade XW.Finishing was carried out under the supervision of occlusion copy paper 8 microns. Polishing using abrasive discs «Sof-Lex», 3M ESPE (vestibular surface), rubber and silicone heads (palatal surface). Control of the contact surface floss.

Results and discussion. After a week and a month after sealing as a result of physical examination found no violation of fit of the composite, good adhesion to the material hypoplastic enamel during the probe along the border seal \ enamel probe slid smoothly without delays, occlusal relationship without violating, preservation of aesthetic properties, the maximum color match composite enamel.

Conclusions. Based on the results of clinical application of nano-filled composite Filtek Ultimate for the restoration of anterior teeth with enamel hypoplasia patchy form, it can be concluded about the good aesthetic properties of the material, ease of use, high strength and duration of the wear resistance of the material, durable marginal seal. A series of follow-up visits will determine the long-term results of treatment.