Movchan O.V.,

KhNMU, orthopedic dentistry department, assistent

Comparative analyze quality and qualimetric evaluation of adhesives materials to improve for the fixation of the removable dentures

The need for adult population of Ukraine in complete removable dentures is considerable and is 57.5 people (77.35 dentures) in 1000 examined. Complete absence teeth already registered in the age group 45-49 years, accounting for as a whole 6,3 ± 0,67% cases per 100 examined. Thus, the number of jaws with complete absence teeth and adverse anatomical-topographic conditions of prosthetic plate, reaches 87.1% of their total number (15.1% of the upper and 72.0% of the lower jaws). The total lack of teeth causes psychological, personality changes, violates social tolerance, changing nutrition. To date do not have perfect method of orthopedic treatment, which would give a guaranteed fixation of denture on Edentulous lower jaw, especially in cases of sudden atrophy or other of relief numerous changes of the oral mucosa. Using of adhesive means significantly increase the efficiency of fixation and stabilization of complete plastic dentures in adverse anatomical-topographic conditions of the masticatory apparatus. They increase the functional value not only manufactured again, but the old dentures also, reduce displacement of a denture on prosthetic plate, stopped excess of the food inside the dentures, it is causes, why complete removable dentures is comfortable.

By research quality characteristics was developed and introduced into production in JSC "Stoma" new adhesive material "Stomafix" for fixation of removable dentures.

Purpose of research - advisability clinical application of adhesive materials and learning on the basis experimental justification of physical and mechanical properties according to the requirements ISO-10873: 2010 and qualimetric evaluation of the quality materials.

Materials and methods.

Comparative analysis of the quality adhesive materials for improving fixation of removable dentures and chewing efficiency, and reducing the period of adaptation clinical exploitation included generalizing results for the laboratory study of the properties following materials: "Stomafix" JSC "Stoma" (Kharkov, Ukraine), «Corega» («Stafford Miller", Ireland), and «Lacalut» («Arkam GmbH", Germany), which provides ISO-10873: 2010: consistence, tensile strength, solubility, adhesion with plastic, metal adhesion, viscosity relative.

Research results.

By the indicator consistency, all materials meet the requirements of ISO-10873: 2010 and substantially (p≤0,05) do not differ among themselves. Thus, the investigated materials are characterized by a slight reserve compared to the indicative index.

Tensile strength samples from adhesive materials exceeds the relevant indicative value of ISO-10873: 2010 to (50 ч 60) %, except material «Lacalut», which as we know can reduce the quality of adhesion and influence the timing of its clinical use.

Solubility adhesive materials characterized by the largest (p≤0,001) for material «Lacalut» - (41,5 ± 0,9) mm / h, while materials "Stomafix» - (35,8 ± 0,6) mm / h and «Corega» - (35,5 ± 0,8) mm / h in this property do not exceed and indicative index, same time are significantly lower than for the material «Lacalut».

By the indicator adhesion with plastic, the investigated materials by 40-45% higher than the indicative value of ISO-10873: 2010 that is able provide more base strength under dynamic loads.

By the indicator adhesion to metal the investigated materials by 25-30% higher than the indicative value of ISO-10873: 2010 that increase the cohesion of metal base removable denture with mucosa.

Viscosity relative at the time of application of the adhesive material varies within (62,0-68,3) s and is the lowest in the case of materal «Lacalut» - (62,0 ± 0,6) s, and largest for the material «Corega» - (68,3 ± 0 2) s, p≥0,05.

Conclusion.

Thus, based on the aforementioned comparative research adhesive materials for increasing the fixation of complete dentures can be concluded that according indicators ISO-10873: 2010, that is consistence, tensile strength, solubility, adhesion with plastic, metal adhesion, viscosity relative adhesive material "Stomafix" JSC "Stoma" (Kharkov, Ukraine) exceeds the indicative value of foreign analogues «Corega» («Staford Miller", Ireland) and «Lacalut» («Arkam GmbH", Germany), the expense of what there is increasing chewing pressure and reduce the period of adaptation of patients to of complete dentures. Research data allow to recommend "Stomafix" JSC "Stoma" (Kharkov, Ukraine) in clinical prosthodontics.

List of references:

1.	Лабунец В.А. Клинические сочетания съёмных зубных протезов / В.А. Лабунец, Т.В. Диева // Акт. пробл. ортопед. стоматол. та ортодонтії: Матер. Всеукр. наук. практ. конф., 11-18 трав., 2000 р. – Полтава. – Вип.2. – С. 15-27.

2.	Макаров Ю.П. Розміри та взаємовідносини беззубих щелеп у геронтологічних пацієнтів // Український науковий медичний молодіжний журнал, 2005. –№ 4. –С. 58-61.

3.	Голик В.П., Янишен И.В., Фадеева С.О. Изучение клинической эффективности применения кремов для фиксации съемных пластиночных протезов: материалы международной научно-практической конференции «Инновационные технологии в стоматологии и челюстно-лицевой хирургии», - Харьков, 2009. – С. 266.