Dentures quality at the stages of its clinical durability

Kozitskaya О.І., Yanishen I.V.

Kharkiv Medical Academy Postgraduat , Health Ministry of Ukraine

KharkivNationalUniversityof Public Health Ministry of Ukraine

The purpose of the research was aimed at comparative analysis of quality of fixed dentures at the stages of its clinical durability.

Materials and Methods. The results of expert evaluation, performed in compliance with f.043/о in 10 medioprophilactic institutions comprised the following mode of dataware:  the total amount of studied fixed dentures was 35950 pieces. The comparative quality assessment of 20329 artificial crowns, 15621 bridge dentures has been made at the stages of clinical durability of prosthetic appliances.

Results. Time periods and signs of decrease in quality of plastic and combined artificial crowns have been studied. The study showed that quality of artificial crowns is defined by the length of dentures’ clinical durability and their type. So, at the early stage of clinical durability artificial crowns are characterized by the higher level of quality, than combined ones (р<0,05), which depends on overall rate of specific signs of decrease in  quality of the appliances (р<0,01) and ratio of prosthetic appliances with the signs of quality decrease. In the remote period of clinical durability plastic crowns are characterized by more apparent decrease in quality level of prosthetic appliance than combined ones (р<0,05), which occurs, first of all, due to increase of the overall rate of individual signs of decrease in quality of appliance (р<0,01). The quality of bridge dentures depends on different reasons and is also defined by the length of clinical durability of the appliance.

Conclusions. The technique of comparative analysis of quality of fixed dentures has been studied and implemented at the stages of clinical durability of plastic and combined artificial crowns and bridge dentures according to the range of indices. It has been proved by evidence, that quality of artificial crowns is defined by the length of clinical durability of the appliance and is significantly higher, than the quality of combined ones at the early stage of their clinical durability; at the same time in the remote period of clinical durability plastic crowns are characterized by higher rates of quality index.